University of the Arts London

# Central Saint Martins College of Art & Design

School of Graphic & Industrial Design

Clay Preparation and Testing

Clay is a widely occurring material, commonly found in the banks of rivers and streams or in the exposed layers of road cuttings. Once you find a clay deposit you can test to see if it can be used for making pots by picking up a handful and squeezing it in the palm of your hand.
If it crumbles it is probably not plastic enough, If it holds together it is likely that it can be used, so dig a bucket full. When you dig your own clay there is likely to be debris such as stones, roots and grit.

Preparation:

- In order to clean the clay, break up larger lumps, spread it out and let it dry. When dry use a wooden mallet to further break it up.

- Add the dry clay to a bucket of water; use twice as much water as clay.

- Let it dissolve and settle for a few hours or overnight.

- Strain it through a 40-mesh sieve.

- Let it settle for a few more hours and then pour off the excess water from the top.

- It is now the consistency of thick slip so pour it out onto a big plaster of Paris block so it can dry to a working consistency and then it will be ready to wedge.

Tip: To prevent potential contamination of the clay with plaster, spread the clay on a sheet of canvas laid on the plaster block.

You may be lucky to find that the clay is of a good workable quality, suitable for purpose. However, clay with properties suitable for slip casting may not be appropriate for large sculptural work. It is therefore worth testing clay prior to use.

Note: This applies to both natural and prepared clays.

What is being tested?

- Shrinkage

- Plasticity

- Slumping and firing temperature

- Porosity

Shrinkage:

Clay shrinks in 3 stages. First when it dries out; second when it is bisque fired and third when it is fired to its top temperature (usually the glaze temperature).

- Prepare some 5mm thick slabs of clay 120 X 40mm

- Scribe a 100mm line down the centre

- Measure the length of the line after it has dried, after bisque firing then after firing to top temperature

Plasticity:

Different levels of plasticity are required for different applications. Throwers require clay with strength and elasticity, so clay producers manufacture a range of clays specifically formulated for that purpose. If you are adapting natural clay, plasticity can be increased by the addition of ball clay or Bentonite.

To test for plasticity simply roll out a small coil of clay and bend it into a tight loop. Non-plastic clays will split and open easily, whilst plastic clays will bend without any sign of cracking.

To increase plasticity it is simplest to add ball clay or Bentonite to clay slurry. As natural clays vary there are no rules to the amount of material to add. The correct amount will only be ascertained after testing.

Slumping:

The higher the temperature that the clay is taken to, the more likely it is to deform. This is because the materials become more like glass (or glaze) and are therefore more fluid.

| To check for slumping take a dried test strip and put it across two previously fired slabs that are stood on edge. Fire a number of test strips to a range of temperatures. Once you have found the maximum firing temperature, try a glaze firing in that range to check how the glaze fits the clay. * |  |
| --- | --- |

*Note: Repeated firing has an accumulative effect. (The clay has experienced more heat work than clay fired once or twice.)

Porosity:

Generally, earthenware clays tend to be porous, stoneware, porcelain and bone china are normally non-porous.

The difference is achieved through vitrification. Vitrification is the process of melting that clays and glazes go through as they are fired to maturity. In a fully matured clay body, the spaces between refractory particles are completely filled up with glass, fusing the particles together and making the clay body impervious to water.

Earthenware pots need to be glazed to make them watertight, whereas porcelain and bone china can be left unglazed. (See Sacha Wardell’s bone china pots.)

Materials:

Clays are classified into plastics, including ball-clays and china clays, and non-plastics, including ground flint (more properly ground quartz), ground feldspar, limestone, talc, etc. Shrinkage is greater in the plastics than the non-plastics.

Ball clays approach the theoretical formula for ideal clay Al203, 2SiO2, 2H20, but containing fusible impurities, they vitrify at lower temperatures than china clays. Ball-clays are very plastic.

China clays or kaolins are the nearest to the formula above. They are used to give whiteness to a pottery body and to raise its firing point. Kaolin is the chief plastic ingredient in porcelain, but because its plasticity is much inferior to that of ball-clays, a porcelain body is nearly always short and difficult to handle on the wheel.

Flint (SiO2) is used to raise the firing point of a body, to open it up where it is too "fat" or "tight," whiten it, and increase its coefficient of expansion. The addition of flint to a body, while actually de-creasing its plasticity, may make it easier to work by "opening it up." Where a glaze cracks or "crazes" because it shrinks more than the body on which it is applied, the addition of flint to the body will make the body shrink more (this refers to the shrinkage that takes place on cooling, not the drying or firing shrinkage), and the glaze will fit it better.

Feldspar (K20, 2Al203, 6SiO2) like flint opens up a body in the raw clay. It increases the firing shrinkage, because it melts and runs down between the particles of flint and kaolin cementing them together as a glassy flux. This vitrifying effect is complete only at high temperatures.

Whiting (CaCO3) is ground marble or limestone and is frequently used up to about 10% to whiten a body and make it dense. It lowers the firing point of the body.

Talc is used to toughen bodies and lower their firing points. It may tend, however, to shorten the firing range.

Bentonite is fine colloidal clay that swells up to several times its own volume when added to water. About 7% of the weight of water will make a very stiff jelly. It is useful to add to clays that are "short" to make them more plastic.

Typical Recipes:

|  | Earthenware |  |  | Stoneware |  | Porcelain |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Recipe | 1 | 2 | 3 | 1 | 2 | 1 | 2 |
| Ingredients | % | % | % | % | % | % | % |
| Ball clay | 65 | 30 | 48 | 25 | 35 |  |  |
| China clay | 14 | 20 | 25 | 25 | 20 | 55 | 50 |
| Flint | 11 | 35 | 4 |  |  |  |  |
| Whiting | 10 |  |  |  |  |  | 8 |
| China stone |  | 15 | 23 | 25 |  |  | 25 |
| Sand (silver) |  |  |  | 25 |  |  |  |
| Feldspar |  |  |  |  | 20 | 25 |  |
| Bentonite |  |  |  |  |  | 5 |  |
| Quarrtz |  |  |  |  |  | 15 |  |
| Firing Temp | 1080° - 1120°C |  |  | 1260° - 1280°C |  | 1280° - 1320°C |  |

Clay Additives:

In addition to the materials detailed above there are a number of other materials that can be added to improve the properties of the clay or to create decorative effects.

Ceramic Additives:

Grog is made from ground up fired clay and is one of the most common additions to clay, It makes excellent filler because it reduces shrinkage, provides throwing strength, and minimizes warping and cracking. Available in various grades, it can be added (up to 20%) to the dry clay body ingredients, to clay slurry or thoroughly wedged (after wetting) into plastic clay.

Clay manufactured for large sculptural work often contains considerable amounts of coarse grog making the clay highly textured.

Molochite is a good substitute for grog, especially where a clay body is intended to remain white. (An important ingredient in T- Material)

Grit and Aggregate can be added to produce a heavy textured clay suitable for sculpture. Some particles will melt, whilst others will remain granular.

Feldspar produces beautiful soft eruptions of melted glass when large particles are kneaded into stoneware clay.

Non-ceramic Additives:

| Natural materials can be added to clay in order to create interesting surface texture. For example, rice has been added to porcelain, producing a translucent pattern. Pasta, pulses and grains are also suitable for adding to clay. Avoid adding plastics to clay as a toxic gas will be produced on combustion. |  |
| --- | --- |

Michael Eden 2011

For details of London Clay see: http://en.wikipedia.org/wiki/London_Clay

‘Heat work’ is the term used to describe the amount of heat that a clay body or glaze receives during a firing. The measurement of heat work is a more accurate method than temperature measurement. A long slow firing needs to achieve a lower temperature than a short, fast firing. Heat work can be measured by the use of ‘cones’ visible through the spyhole of the kiln. They are formulated to deform then melt after a certain period in the kiln. Therefore, if a glaze has been formulated to mature at 1100°C an 03 cone will melt at exactly the correct point. The person firing the kiln will then know when to switch it off.

Clark, Kenneth. The Potter’s Manual. P12

See the work of David Binns - http://www.davidbinnsceramics.com/

See the ‘Trinary’ pieces by Koji Shiraya - http://www.kojishiraya.com