University of the Arts London

# Central Saint Martins College of Art & Design

School of Graphic & Industrial Design

# BA Hons Ceramic Design

# Clay

Introduction:

The history of Humankind can be traced through the ceramics that fill our museums. From 10,000+ years old Jōmon pottery to high-tech ceramic knives, clay has been a fundamental building block in the development of complex societies. Literally!

| Jōmon pottery | Brick wall | Ceramic knives |
| --- | --- | --- |

But why?

It is one of the most widely available raw materials available in the world and can be one of the least expensive to mine and prepare for use. Dig down under this building (and most of south-east England) and you will find good quality, useful clay. You will normally see clay where roads are cut through hillsides and in the banks of streams and rivers.

What is it and how did it get there?

Most clay began as rock, broken down and decomposed by millions of years of weathering.

There are two types of naturally occurring clays: Primary (or residual) and Secondary (or sedimentary).

Primary Clay is found close to the source rock from which it was formed. These are less common than Secondary Clays but include China Clay (kaolin)

Secondary Clays are formed when rivers carry away primary clays and deposit them in sedimentary layers. This action has the effect of grinding the material into finer particles and adding impurities along the way. For instance, Ball Clay, found in large deposits in southwest England is often blue or black in colour (firing to buff or off-white) due to the presence of decomposed vegetable matter.

Red Earthenware is also secondary clay, stained by iron oxide, a very commonly occurring mineral colouring agent. Smooth and often very plastic, it has a low firing temperature, making it a versatile material, used to form vessels, bricks, religious artefacts etc.

Another secondary clay is Fireclay, named because it is usually found near coal deposits. Its properties are very different to Red Earthenware; it is coarse in texture, pale in colour and high firing.

Natural Clays

As I have just mentioned, Red Earthenware is the most widely found natural clay. Find any pottery site on old maps and you can be sure that the site was chosen due to its proximity to raw materials- clay and a reliable firing material (wood or coal). Stoke-on-Trent developed as a pottery manufacturing area due to the availability of different clay types, coal and other useful minerals.

Potteries were rarely sited close to Primary clay sources, as they are mostly unsuitable.

Prepared Clays

Primary clays such as China Clay cannot practically be used to form ceramic objects, as they are composed of pure, larger sized particles. They need to be combined with other, more plastic clays, such as Ball Clay or Bentonite in order to make them useful.

Clay Properties

When we create a ceramic object the appropriate materials must be chosen. Each type of clay has particular properties including colour, texture, firing temperature and strength. I may choose particular clay because of the decorative technique I wish to use, but prepared clays have been developed primarily for practical reasons. For instance, earthenware casting slip is normally white (suitable background for a range of decorative techniques), lower firing (saves energy) and strong enough for everyday functional pottery.

Clay Types

Earthenware Clay:

Has been used throughout the world from the earliest times. The commonest type is terracotta (Italian for ‘fired earth’); it is used to make a wide variety of products including roof tiles, drainage pipes and bricks as well as functional, domestic pottery. It is usually fired between 950 and 1120ºC. Traditionally terracotta clay has been used for cooking pots as it has good thermal properties and some clay bodies will withstand use on an open fire. Additions of sand or grog give the clay more strength, making it easier to retain its shape and more resistant to glaze crazing.

White Earthenware is made primarily from Ball Clays, is usually smooth and unsuitable to forming by hand. Developed for use in industry is lends itself to the production of large volume, decorated domestic ware.

Stoneware Clay:

The majority of stoneware clays are manufactured from a mixture of raw materials, which can include Ball Clay, China Clay, Bentonite, sand or grog. Fireclay is naturally occurring stoneware clay, generally used to produce grog when ground and fired. As Stoneware clay fires to a higher temperature range than Earthenware – 1240 - 1280ºC, it is normally non-porous and vitrified. As a result it is stronger than Earthenware and therefore suited to outdoor uses, as well as in the production of functional domestic ware.

Porcelain:

Porcelain is a prepared clay, generally believed to have originated in China. It is extremely hard, white and has a translucent quality. Mostly comprised of a mixture of China Clay (kaolin), and feldspar it is generally fired between 1280 and 1320ºC, which makes it suitable for table, kitchen, sanitary, and decorative wares; objects of fine art; and tiles. Dental porcelain is used to make false teeth, caps, crowns and veneers. Porcelain also makes an excellent electrical insulator.

Bone China:

Bone China was invented as a result of Pottery manufacturers attempts to imitate fashionable porcelain that was being imported by the shipload from the Far East. Made from a mixture of bone ash (up to 50%), China Clay, feldspar and quartz, it is generally fired to 1280ºC. Pure white and translucent, it lends itself to the production of high quality table ware. As it has poor mechanical strength before firing, it is usual to give objects that are intended to remain unglazed a low temperature biscuit firing (650-800ºC) after which pieces soaked in water can be polished with wet and dry paper.

In addition the clays listed above there are also clay bodies formulated for specific purposes or conditions, such as Raku where thermal shock needs to be allowed for and Paper Clay, a prepared mixture of shredded paper and clay, ideally suited for the construction of large scale and delicate sculptural ceramics.

A wide variety of clay bodies are available from a number of suppliers; before ordering large quantities it is wise to test a number of samples in order to find the one most suitable. Most suppliers will provide free samples on request.

Rough Guide to Clay Types

|  | Earthenware | Stoneware | Porcelain | Bone China |
| --- | --- | --- | --- | --- |
| Firing temp. | 950 - 1120ºC. | 1240 - 1280ºC, | 1280 -1320ºC | 1260 - 1280ºC |
| Decoration | Slips, clear or translucent glaze; Opaque glaze with oxide decoration (Majolica, Delft) Transfers | Clear, translucent or opaque glaze. | No Glaze; Clear, translucent or opaque glaze. | No Glaze; Clear, translucent or opaque glaze. Transfers |
| Forming techniques | Coiling, pinching, throwing, casting | Coiling, pinching, throwing, | Throwing, slipcasting | Slipcasting |
| Uses | Domestic functional ware; ceremonial/religious; decorative; building - bricks, pipes, tiles | Domestic functional ware; decorative; | Domestic functional ware; decorative; Industrial – e.g. acid resistant containers; | Domestic functional ware; |

Examples

| terracotta cooking stove | medieval pitcher | tin glazed earthenware |
| --- | --- | --- |
| wood fired stoneware | stoneware glaze tests | Bodil Manz porcelain |

| Matthew Blakeley celadon glazed porcelain | slip cast porcelain by Ionna Vautrin |
| --- | --- |
| Bone China teacups and saucers | Bone China bowl by Sacha Wardell |

As technology has advanced the properties of refined clay materials are being increasingly exploited.

Zirconia, Aluminium nitride and steatite are just a few examples of refined ceramic materials found in an ever-increasing variety of applications.

| Rado Watch | Make-up | Spark Plug |
| --- | --- | --- |

| Guitar | Circuit Board | Ceramic Coil |
| --- | --- | --- |

Further Reading

Scott, Marylin. ‘The Potter’s Bible’, Chartwell Books Inc. 2006

Hamer, Frank and Janet. ‘The Potter’s Dictionary’, A & C Black 2004

Clark, Kenneth. ‘The Potter’s Manual’. Chartwell Books Inc

Lefteri, Chris. ‘Ceramics, Materials for Inspirational Design’. Rotovision 2003

Michael Eden 2011

www.potclays.co.uk (catalogues and technical information can be downloaded from the Library section of the site, via Support/Downloads) | www.valentineclays.co.uk | www.scarvapottery.com | www.pottersconnection.com

See: Lefteri, Chris. ‘Ceramics, Materials for Inspirational Design’. Rotovision 2003