University of the Arts London

# Central Saint Martins College of Art & Design

School of Graphic & Industrial Design

# CLAY.

Clay is the most fundamental material used by the potter.  It is one of the most widely available raw materials available in the world and can be one of the least expensive to mine and prepare for use.

“Clay may be defined as an earthy mineral substance, composed largely of a hydrous silicate of alumina, which becomes plastic when wet and hard and rock-like when fired”.  Daniel Rhodes.

Five minerals constitute about 90% of the surface of the earth. Of these, Silica 60% and Alumina 15% are by far the largest, together with smaller quantities of iron, calcium, sodium, magnesium, potassium, water and titanium.

PRIMARY CLAYS.

The basic clay substance, also known as “KAOLINITE” has the chemical composition

Al 2 O3 (Alumina).  2 SiO2 (Silica). 2H2O (Water).

It is formed from the decomposition of igneous felspathic rocks – granite and basalt - by the action of water - “weathering” over a period of many thousands of years.

Most of the decomposed material – clay - is washed away from the rock by the action of water. The clays discovered near their source are described as “PRIMARY CLAYS” the best known being called “CHINA CLAY” or “KAOLIN”.

China clay tends to be pure and white and, although it may feel smooth to the touch, it has comparatively large, plate-like particles, which makes it fairly non- plastic for use in pottery forming.

“PLASTICITY” - in the context of forming clay - relates to the clay’s ability, when softened and lubricated by water, to be pushed and stretched into controllable forms which will remain and become permanent after the clay has dried out.

China clay is a very useful ingredient in high-fired clay bodies such as porcelain, where its whiteness and purity and ability to withstand very high temperatures is valued. It is normally necessary to blend it with other, more plastic clays to improve its workability.

SECONDARY CLAYS.

Much clay is transported, especially by rivers, away from its source and deposited, often a great distance from its origins.

This is known as “SECONDARY CLAY” and is characterised by greater plasticity due to the particle size having been ground down by constant movement in the water.

The process of transportation also gives it a good chance of becoming affected by other minerals and organic matter, leading to the clay becoming coloured, the strength of colour varies.

The commonest colourant is Iron Oxide which makes it buff or brown coloured dependent on the amount present.

Iron oxide is also known as a “Flux” which means that its presence causes the clay to begin to melt at a lower temperature than a purer clay like kaolin.

There are many types of secondary clay deposited in seams of varying size and depth and the individual clay deposits possessing different physical qualities.

Some of the most useful types of clay for use in ceramics are known as

“BALL CLAYS”.

These were so called because in the 18th century, before the widespread development of canals for industrial transportation, large balls of these clays were placed on the backs of packhorses for carrying from the clay mine to the pottery. (The potteries tended to be located near to coalmines for easy access to fuel for the kilns and specialist clays and other raw materials sometimes had to be imported from elsewhere).

Ball clays vary in colour when fired from off-white to buff depending on how much iron oxide they have picked up on their journey.

Before firing, ball clays can vary greatly in colour due to varying amounts of organic matter present. Whilst this can add to the plasticity of the clay when wet, it burns away during firing, leaving little trace of its colour in the raw state.

(For example, “Black Ball Clay” fires whiter than the slightly more plastic “Blue Ball Clay”).

Ball clays tend to be too plastic to be used on their own and shrink too much from the soft to dry states. In order to produce a well balanced clay ”body” a blend must be made with other less plastic ingredients such as kaolin and “fillers”.

FIRECLAYS.

A group of clays which were deposited in ancient woodlands which have turned into coal – the clay is sandwiched between coal seams.

Fireclays tend to be coarse grained, containing much organic matter, free quartz, calcium, mica and speckled with iron. They are refractory (able to withstand high temperatures). Alumina content 10-40%, Silica 40-80%.

Useful for making GROG (a granular fired clay filler for plastic bodies),

Bricks (especially “Firebricks” used in kiln building), crucibles, kiln furniture.

Added to smoother clay bodies they provide texture, refractoriness and physical strength and those higher in iron oxide bring specks of metallic colour

COMMON CLAYS and MARLS.

These clays are to be found very widely throughout the world normally just under the topsoil or in the beds of rivers and streams. After firing they are generally coloured buff to red brown from iron oxide. When found the clay may look cream, grey, orange, black or khaki due to the organic matter which burns away in the kiln.

For many centuries these clays have been gained from opencast mining and form the unrefined raw material for countless numbers of terracotta wares such as building bricks and tiles, flowerpots, country earthenware pottery etc.

## BENTONITE

An extremely fine-grained super plastic “clay”, Bentonite is formed from decomposed volcanic ash and is one of a group of minerals known as “montmorillonites”.

The plasticity of a clay body can be dramatically increased by the addition of up to 6% and small quantities added to a glaze mix can improve the suspension of materials in the water.

PREPARED CLAY BODIES.

We have taken a very superficial look at the basic clay types.

Clay bodies that are used for ceramics are generally a blend of a variety of ingredients.

Qualities sought by the ceramist relate to plasticity, workability, fired stability and strength, texture, colour, maturing temperature etc.

“The development of a reliable ceramic body which matures in the desired temperature range and has the appropriate handling qualities for the forming methods to be used, as well as having the desired fired appearance and texture, is not always an easy task.”  Rich Slade.

The composition of a ceramic body can be said to comprise: clay, flux, and filler.

Refractory clays such as china clay and fireclay can be made to “mature” at a lower temperature by the addition of fluxes. “Maturing” means the formation of a compact, almost glass-like structure within the body. This causes the body to develop its optimum strength and to become comparatively impervious.

Common clays with a high iron content (about 10%) mature at a fairly low temperature due to the fluxing effect of the iron oxide whilst paler bodies tend to need a higher firing temperature to achieve the same degree of “maturity”.

There are a large number of specialist clay bodies available for the ceramist to choose from.  The range covers a wide variety of colours, textures and fired characteristics.  On this course we can only afford to provide, free of charge, a very limited number of different clays (but these can be modified by the individual to suit their own needs).

It is vital to fire clay to the optimum temperature for the characteristics one wants to exploit. By standardising clay types and kiln firing temperatures we attempt to use our resources as efficiently and economically as possible.

One of the great things about clay is that, even if it has dried out (for example after an unsuccessful attempt at building a coil pot) it can be soaked in water - which turns it once more into an amorphous, sticky mass – and may be reconstituted and used again and again until the result is suitable for firing.

Processing clay for ceramic forming entails a good deal of physical work, either mechanically by passing it through a PUGMILL (which extrudes the mixed clay out as a long sausage) or by hand.  Hand blending, known as

“WEDGING” or “KNEADING” is a laborious prelude to throwing and other hand forming processes but is an important activity to ensure that the clay is in good condition for forming.

The “workability” of clay can be improved by ageing. If a clay body has been used a lot and is “tired”, or if it has just been blended for the first time, it will benefit from being stored, damp, in a pile, wrapped in polythene. This can increase plasticity. It has been said that traditionally, in China, potters mixed and stored clay for their grandchildren to use.  Even a few days storage will help to restore a tired pile of wheel thrown pots that “didn’t quite make it”, so that one week’s failures can become the next week’s successes.

One way of categorising ceramic ware, regardless of form, function or the maker’s intention as to its visual identity is into these loose definitions:

EARTHENWARE.

This tends to be defined by the fact that, in ceramic terms, it is fired to a fairly low temperature and that, even after glazing, the clay body remains porous.

Earthenware is the soft “terra cotta” (Italian for “fired earth). It is the common red brown house bricks and tiles found all over the world.  As described before, this red brown colour is due to an iron content of up to 10%.

Earthenware may be white or buff or may be stained any number of other colours. It may be burnished and polished and fired to only 900ºC (Celsius or centigrade) thus remaining very soft, but having a subtle sheen like the work from many technologically primitive peoples or ancient civilisations.

Alternatively, it may be decorated with slips or underglaze colours and glazed with clear or opaque lead or alkaline glazes.

On this course, to introduce students to the disciplines of firing and glazing ceramics, we start by working at earthenware temperatures.

The two most commonly used clays on the course, “GROGGED BUFF” and “WHITE EARTHENWARE” are “BISQUE” fired at 1140 – 1160ºC and then GLAZE fired at 1060 – 1100ºC.

STONEWARE, PORCELAIN and BONE CHINA

Fired to a substantially higher temperature, wares described as “STONEWARE” are inclined to be pale in colour and, essentially, they have developed glass- like characteristics which means that they have become vitreous, - impervious to water, - even if not covered with glaze.

“PORCELAIN” and “BONE CHINA” are closely related to stoneware in firing range and are generally pure white (more or less) and have the added affinity with glass in that, when thinly constructed, show a degree of translucency when held up to light.

Wares in Stoneware, Porcelain and Bone China are generally given a fairly low bisque firing, followed by a glaze firing of 1250 – 1300ºC.

If it is decided not to glaze the ware, then it may be fired once only to the top temperature for vitrification.

Due to the high temperatures leading to the ware being on the verge of melting, the designer must ensure that the form is very strong, or the work needs to be supported in a sort of ceramic cradle or “setter” to ensure that it does not collapse during the final stages of the firing.

BISQUE FIRING

When firing any clay article, it is vital to check that it is completely physically dry.

Plastic clay contains chemically combined water and also the so-called “water of plasticity”,  – the water that lubricates the clay particles and enables one to manipulate and form the clay.

As the clay article dries, the water of plasticity evaporates and the platelets which make up the substance of the clay settle closer together causing the article to shrink.

Even if the clay appears to be completely dry, there are always little pockets of water which have not evaporated and this is known as “pore water.”

Water boils at 100ºC. so the firing should be started very slowly as water expands when it becomes steam and, if this happens too rapidly, it could cause cracking or explosion of the article. The kiln should be well ventilated at this stage.

The next drama that occurs in the clay body is called the “Cristobalite Squeeze” at 226ºC.  This refers to a sudden contraction of the ware due to silica in the clay substance converting from “Alpha Cristobalite” to “Beta Cristobalite”.  Later, at 573ºC., a quartz inversion between its alpha and beta forms causes an expansion by 3.5%.

All this adds up to the need to heat up slowly and, as the alpha/beta inversion is reversed on cooling, it is important not to open up the kiln too soon at the end of the firing to avoid cracking the ware at that stage of events.

The firing proceeds slowly after the steam has been given off because the next stage is the irreversible conversion of the clay to ceramic between about 450 and 600ºC.    This is known as “CERAMIC CHANGE” and, although the article would still be extremely weak and “underfired”, it would never convert back to soft sticky clay, however long it was soaked in water.

Having got past these obstacles, the firing may be speeded up somewhat.

(You will be taught how to programme the kiln controllers to follow a safe path of controlled temperature rise to suit the kind of work you are firing).

Having established that the heat applied to the work has irreversibly turned it from clay to ceramic, you now have the choice as to the top temperature that you want the work fired to.

If your work is to be glazed EARTHENWARE, then it needs this initial “BISQUE” firing to be high enough to ensure that the body is strong and not too porous. This is a critical judgement because, if the work is fired too high it will become very difficult, subsequently, to apply a glaze (which is effectively powdered glass, mixed with water), as this needs some body porosity in order to adhere to the surface.

Especially if the ware is to be functional and durable, it is probably necessary to bisque fire to at least 1140ºC with a lower temperature for the glaze firing.                                                                                                                                                               It is sometimes important to support delicate forms (even earthenware) to avoid warping during this initial firing. For example, a wide thrown dish is probably best bisque fired upside down, resting on its rim to keep it flat.

Subsequently, when glaze fired to a lower temperature, it is unlikely to warp.

If the bisque temperature is too high and the body becomes too vitreous, then when you come to glaze it, the glaze will just run off the surface and not adhere sufficiently thickly to form an adequately glazed finish.

Later in the course you might be involved with producing stoneware or porcelain wares.  The bisque temperature for these could, if you choose, be lower than that for earthenware, as the work will ultimately be fired to a much higher temperature to mature both body and glaze.

Having reached the maximum temperature chosen for the bisque firing, the kiln automatically turns off.  It is then necessary for you to wait until the temperature has reduced sufficiently for you to open the door to get your work out.

Because of the heavily insulated nature of the kiln construction, it takes a long time to cool down (normally, at least overnight and sometimes 24 hours or more).  This is to ensure the safety of the wares inside.

If the work were allowed to cool too quickly (especially in the later stages of cooling) there would be the danger of cracking (known as “DUNTING”).

John Chipperfield